Technical Data Sheet

NECAL 1330FP PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

NECAL  1330FP is a foam supported pressure sensitive adhesive.

FEATURES

NECAL 1330FP is a lightweight, conformable pressure sensitive tape for window flashing and housewrap film splicing.

PHYSICAL PROPERTIES

Composition:	Rubber based

Release Liner:	W Liner

Thickness:	30 mil +/- 10%

Scrim:		White Polyethylene Foam

PEEL

180 degree peel 	15 min.		16 hrs

PSTC 1 lbs/in.

ABS		5.4 lbs			1.2 lbs (1) (3)

Stainless		5.1 lbs			1.1 lbs (1) (3)

Tyvek Room Temp	3.2 lbs			1.5 lbs (2) (3)

Tyvek 20°F. 	2.2 lbs			1.4 lbs (2) (3) (4)

2 mil polyester to ABS	5.2 lbs			6.6 lbs

SHEAR

PSTC  7	 	1000 grams/in		2000 grams/in		3000 grams/in

>336 hrs (3) (5)		>336 hrs (3) (5)		>168 hrs (3) (5)

(1)  Foam split failure

(2)  Tyvek split failure

(3)  All samples reinforced with 2 mil polyester film as test values exceeded foam strength.

(4)  Samples bonded at 20ºF, left at 20°F for 15 min. then tested at room temp.

(5)  Samples were taken down, had not failed and showed little or no movement.

PERMEABILITY

Water vapor transmission rate:	.04 or less grams per hour

Water absorption:	200 or less grams per square meter

Permeability is based on foam material only without adhesive.  Testing with adhesive would reduce water vapor and absorption considerably.

SURFACE PREPARATION

All surfaces must be dry, smooth, and free of dust, dirt, and debris.  Any loose debris must be cleaned off before application.

APPLICATION

Cut pieces to be adhered to length.  Remove release liner, position and smooth into place from one end to the other eliminating as many air pockets as possible.  Apply based on local code and or standard building practices.  Overlaps should be a minimum of 2 inches.

STORAGE DATA

The shelf life of this material is two years when stored in cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION FOR SAMPLES OR ADDITIONAL INFORMATION

JUN-10