Technical Data Sheet

NECAL 3200 REMOVABLE PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

3200 is a supported removable pressure sensitive adhesive that displays good tack and adhesion but is easily removed with no residue from most surfaces.  A permanent adhesive is on one side of the polyester scrim and a removable adhesive is on the opposite side.  The permanent adhesive is intended to be bonded to the appliqué and the removable adhesive is intended to be bonded to the substrate.

PHYSICAL PROPERTIES

Adhesive:						Acrylic (both sides)

Scrim:	 						.5 mil polyester

Adhesive Thickness:					3.5 mils

Adhesion:						10-20 oz./in. (removable)

Temperature Range:					Application:	50°F. Minimum

Service:	0°F. Minimum

120°F. Maximum

Release Liner:						Available with P or W liner

BONDING INSTRUCTIONS

Apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least one year when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

MAY-09