Technical Data Sheet

NECAL 3400 REPOSITIONABLE PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

3400 is a supported film of repositionable pressure sensitive adhesive that displays good tack and adhesion but is easily repositioned with no residue from most surfaces.  A permanent adhesive is on one side of the polyester scrim and a repositionable adhesive is on the opposite side.  The permanent adhesive is intended to be bonded to the appliqué and the repositionable adhesive is intended to be bonded to the substrate.

PHYSICAL PROPERTIES

Composition:						Acrylic (both sides)

Release Liner:						Available with P or W liner

Scrim:							1.0 mil polyester

Adhesive Thickness:			 		5.0 mils (total)

Adhesion: 						200-220 oz./in. (repositionable)

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

195°F. Maximum

BONDING INSTRUCTIONS

Apply to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is at least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

JAN-11