Technical Data Sheet

NECAL 4003 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

4003 is an unsupported film of pressure sensitive adhesive which displays very high tack and superior bond.

FEATURES

4003 will adhere to many substrates.  It will bond to engineering plastics.  4003’s aggressive initial bond builds into a superior bond.

PHYSICAL PROPERTIES

Adhesive:						Acrylic

Release Liner:						P, P1,W,W1

Adhesive Thickness:					1.0 – 2.0 mils dependent upon application

Scrim:							2 mil chrome, 2 mil brush chrome, 1 mil mylar,

2 mil mylar, and 4 mil mylar

Adhesion:						80-100 oz./in.

Tensile:						100 p.s.i.

Shear Adhesion:					7 days +

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

300°F. Maximum

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least one year when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09