Technical Data Sheet

NECAL 4500 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

NECAL 4500 is a high strength, high shear, pressure sensitive adhesive that displays very aggressive initial tack, used only to manufacture label stock.

FEATURES

NECAL 4500 has an excellent adhesion to most substrates, including polyethylene and polypropylene.

PHYSICAL PROPERTIES

Composition:						Rubber base

Release Liner:						Available with P, P1, W, or W1 liners

Thickness:					             1.0 – 2.0 mils dependent upon application

Scrim:							2 mil chrome, 2 mil brush chrome, 1 mil mylar,

2 mil mylar, and 4 mil mylar

Adhesion:						80-100 oz. /in.

40 – 50 oz. /in. to polyethylene and polypropylene

Tensile:						             70 p.s.i.

Shear Adhesion:					7 days +

Temperature Range:					Application:  50°F. Minimum

Service:         -40°F. Minimum

170°F. Maximum

BONDING INSTRUCTIONS

Remove the release liner and apply to a clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with a dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is at least two year when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

Standard UL 969

This material complies with

Component-Marking and Labeling

System Materials (PGGU2).

March-13