Technical Data Sheet

NECAL 4600 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

4600 is an unsupported film of pressure sensitive adhesive displaying high tack and good creep resistance.

FEATURES

4600 will adhere to many substrates, supplied as a bubble free film for backlit applications.

PHYSICAL PROPERTIES

Adhesive:						Acrylic

Release Liner:						P, P1,W,W1

Adhesive Thickness:					1.0 – 4.0 mils dependent upon application

Scrim:							2 mil chrome, 2 mil brush chrome, 1 mil mylar,

2 mil mylar, and 4 mil mylar

Adhesion: (1)						80-85 oz./in.

Tensile: (2)						150 p.s.i.

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

400°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in polyester to SS

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least one year when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09