Technical Data Sheet

NECAL 4700 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

4700 is an unsupported film of pressure sensitive adhesive which displays excellent bond and initial tack.

FEATURES

4700 is designed for bonding to polypropylene and polyethylene.  4700 adheres to many other substrates.

PHYSICAL PROPERTIES

Adhesive:						Modified Acrylic

Release Liner:						P, P1,W,W1

Adhesive Thickness:					1.0 – 4.0 mils dependent upon application

Scrim:							2 mil chrome, 2 mil brush chrome, 1 mil mylar,

2 mil mylar, and 4 mil mylar

Adhesion:						60-75 oz./in. (Aluminum/Polypropylene)

340 – 360 oz./in. (Aluminum/Stainless)

Tensile:						225 p.s.i.

Shear Adhesion:					24 hours +

Temperature Range:					Application:	50°F. Minimum

Service:	-20°F. Minimum

195°F. Maximum

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

AUG 10