Technical Data Sheet

NECAL 5130 HEAT ACTIVATED ADHESIVE

DESCRIPTION

NECAL 5130 is a unique thermoplastic adhesive with excellent bonding characteristics.

FEATURES

NECAL 5130 is designed to be resistant to blocking, so it needs no release liner.  NECAL 5130 has the unique capability of bonding to a wide variety of substrates, including; glass, wood, aluminum, steel, brass, various cloths and leathers, and most plastics (ABS, styrene, nylon, celcon, polyethylene, and polypropylene).  In addition, NECAL 5130 has excellent resistance to water, oil, gas, and most detergents and has excellent low temperature properties.

PHYSICAL PROPERTIES

Adhesion:						Aluminum to ABS 9-14 lbs.

Thickness:					             2.5 mils (total)

Tensile: (1)						300 p.s.i.

Temperature Range:					-60°F. Minimum

190°F. Maximum

(1)  Polyester to SS (1 sq.in.)

BONDING INSTRUCTIONS

Use pressure, 40-60 p.s.i., for 1.5 – 10 seconds dependent upon substrate.  It is essential that the glue line be between 300° - 350°F for bond to develop.  Keep in mind the heat sink effect of the substrate. It may be necessary to preheat the substrate or increase temperature and/or dwell time.

STORAGE DATA

The shelf life of this material is at least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

Standard UL 969

This material complies with

Component-Marking and Labeling

System Materials (PGGU2).

March-13