Technical Data Sheet

NECAL 5132 HEAT ACTIVATED ADHESIVE

DESCRIPTION

5132 is a unique thermoplastic adhesive with excellent bonding characteristics.

FEATURES

5132 is designed to be resistant to blocking, so it needs no release liner.  5132 has the unique capability of bonding to a wide variety of substrates, including; glass, wood, aluminum, steel, brass, various cloths and leathers, and most plastics (ABS, styrene, nylon, celcon, polyethylene, and polypropylene). In addition, 5132 has excellent resistance to water, oil, gas, and most detergents and has excellent low temperature properties.

PHYSICAL PROPERTIES

Adhesion:						Aluminum to ABS 8-12 lbs.

Adhesive Thickness:					1.5 mils

Tensile: (1)						300 p.s.i.

Temperature Range:					-60°F. Minimum

190°F. Maximum

(1)	Polyester to SS (1 sq.in.)

BONDING INSTRUCTIONS

Use pressure, 40-60 p.s.i., for 1.5 – 10 seconds dependent upon substrate.  It is essential that the glue line be between 300° - 350°F for bond to develop.  Keep in mind the heat sink effect of the substrate. It may be necessary to preheat the substrate or increase temperature and/or dwell time.

STORAGE DATA

The shelf life of this material is two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-10