Technical Data Sheet

NECAL 7114 HEAT ACTIVATED ADHESIVE

DESCRIPTION

7114 is a unique unsupported heat activated adhesive.

FEATURES

Necal 7114  displays high bond strengths to many substrates including vinyl, metal, a variety of plastics and various cloths and leathers.  7114 has excellent environmental resistance.

PHYSICAL PROPERTIES

Adhesion:						Cloth & vinyl destroying bond

Adhesive Thickness:					1.0 mil (Total)

Temperature Range:					-40°F. Minimum

200°F. Maximum

BONDING INSTRUCTIONS

Bonding instructions: 4-10 seconds at 325-375°F depending on materials bonded.  Minimum glue line temperature of 300°F and adequate pressure to initiate bonding required.

STORAGE DATA

The shelf life of this material is two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-10