Technical Data Sheet

NECAL 8192 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

NECAL 8192 is a white or black polyethylene foam supported adhesive with superior tack.

FEATURES

NECAL 8192 is primarily intended for applications with extremely rough substrates such as cast iron, cement, etc.  NECAL 8192 has excellent impact and vibration resistance.  NECAL 8192 has excellent adhesion to polyethylene and polypropylene as well as other substrates.

PHYSICAL PROPERTIES

Adhesive:						Rubber based

Release Liner:						Available with P or W liners

Thickness:						32 mils + or – 10%

Scrim:							Black or white polyethylene closed cell foam

Adhesion: (1)						160-170 oz. /in.

80-100 to polyethylene and polypropylene

Tensile: (2)						65 p.s.i., foam failure

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:  50°F. Minimum

Service:         -40°F. Minimum

170°F. Maximum

(1)  PSTC-1

(2)  Polyester to SS (1 sq.in.)

(3)  1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply to a clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with a dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is at least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

March 13