Technical Data Sheet

NECAL 8194-5 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8194-5 is a supported pressure sensitive adhesive that has been designed for high performance requirements in “membrane switch” applications.

FEATURES

8194-5  exhibits excellent diecuttability and shows no adhesive ooze even after extensive aging.  Adhesion is good to most substrates exhibiting repositionability due to lower initial tack but will build to a superior bond after 24-48 hours.  8194-5, with excellent heat, UV and chemical resistance, is recommended for high performance applications.

PHYSICAL PROPERTIES

Adhesive:						Acrylic based adhesive

Release Liner:						P, W, H, HD, VF

Thickness:						5.0 mils (Total)

Scrim:							.001 gauge polyester

Adhesion: (1)						Initial: 80-100 oz./in.  Aged: 170-180 oz./in.

Tensile: (2)						130 p.s.i.

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:	60°F. Minimum

Service:	-40°F. Minimum,

400°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-10