Technical Data Sheet

NECAL 8195 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8195 is a supported pressure sensitive adhesive displaying excellent tack.

FEATURES

8195 will adhere to many substrates.  8195 is highly recommended for rough textured surfaces that have low contact areas.  It can be used where vibration deadening is required.

PHYSICAL PROPERTIES

Composition:						Acrylic

Release Liner:						Available with P or W liner

Thickness:			 			32 mil + or – 10% (Total)

Scrim:							Polyurethane open-celled foam

Adhesion: (1)						95 - 120 oz./in.

Tensile: (2)						90 p.s.i.

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

225°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-10