Technical Data Sheet

NECAL 8197-X PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8197-X is a supported pressure sensitive adhesive that is used exclusively in “soft touch” applications.

FEATURES

8197-X shows no adhesive ooze even after extensive aging.  Adhesion is good to most substrates including aluminum, steel, glass and many plastics including circuit board plastics.  Good initial bond will improve within a few hours or day to a superior bond.

PHYSICAL PROPERTIES

Composition:						Acrylic

Release Liner:						Available with P or W liner

Thickness:			 			1.5 mils on each side

Scrim:							X (indicates total thickness with polyester film.  Example: 8197-7 is a 4 mil

polyester with 1.5 mils adhesive each side.)

Adhesion: (1)						Initial: 100-120 oz./in.       Aged: 170-180 oz./in.

Tensile: (2)						130 p.s.i.

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:	60°F. Minimum

Service:	0°F. Minimum

225°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09