Technical Data Sheet

NECAL 8199-148FP PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8199-148FP is a foam supported pressure sensitive adhesive that exhibits very high performance.

FEATURES

8199-148FP is primarily intended for exterior use where extreme high performance is needed.  An example is exterior automotive.  8199-148FP has superior impact and vibration resistance.

PHYSICAL PROPERTIES

Composition:						Acrylic

Release Liner:						Available with P or W liner

Thickness:			 			143 mils + or – 10%

Scrim:							Black polyurethane foam

Adhesion: 						250-300 oz./in.

Tensile: 						100 p.s.i.

Shear Adhesion: 					7 days +

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

400°F. Max. short term (minutes, hours)

300°F. Max. long term (days, weeks)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09