Technical Data Sheet

NECAL 8493  PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8493 is a supported rubber based pressure sensitive adhesive displaying high tack and good creep resistance.

FEATURES

8493 will adhere to many substrates, including polyethylene and polypropylene.

PHYSICAL PROPERTIES

Composition:						Rubber based

Release Liner:						Available with P or W liner

Thickness:			 			4 mils total

Scrim:							48 gauge polyester

Adhesion: (1)						60 oz./in.

Tensile: (2)						137 p.s.i.

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

170°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09