Technical Data Sheet

NECAL 8502  PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8502 is a supported pressure sensitive adhesive with a general purpose acrylic on one side and a modified acrylic on the other side displaying high tack.

FEATURES

8502 is designed for low energy surfaces (i.e. polyethylene and polypropylene) utilizing the modified acrylic side of the system.  The acrylic side should be bonded to the nameplate only.

PHYSICAL PROPERTIES

Composition:						General purpose acrylic on one side and a modified acrylic

on the other side

Release Liner:						Available with P or W liner

Thickness:			 			4.0 mils (Total)

Scrim:							.00048 mil polyester

Adhesion: (1)						80-100 oz./in. (Aluminum/Polypropylene)

Tensile: (2)						230 p.s.i.

Shear Adhesion: (3)					24 hours +

Temperature Range:					Application:	50°F. Minimum

Service:	-20°F. Minimum

300°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

AUG-10