Technical Data Sheet

NECAL 8608 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

NECAL 8608 is an extremely aggressive supported pressure sensitive adhesive.

FEATURES

NECAL 8608 was designed for adhesion to low energy surfaces (i.e. polyethylene and polypropylene) but especially for rough or textured surfaces.

PHYSICAL PROPERTIES

Composition:						Modified Acrylic (low surface energy)

Release Liner:						Available with P or W liners

Thickness:			 			8 mils (total)

Scrim:							2.0 mils non-woven polyester

Adhesion: (1)						120-150 oz. /in. (Aluminum/Polypropylene)

340-360 oz. /in. (Aluminum/Stainless steel)

Tensile: (2)						250 p.s.i.

Shear Adhesion: (3)					5 days +

Temperature Range:					Application:  50°F. Minimum

Service:         -20°F to 270°F

(1)   PSTC-1

(2)  Polyester to SS (1 sq.in.)

(3)  1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply to a clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with a dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is at least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

March-13