Technical Data Sheet

NECAL 8799-45 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

NECAL 8799-45 is a polyurethane foam supported pressure sensitive adhesive displaying excellent bond and initial tack.

FEATURES

NECAL 8799-45 is designed for polypropylene and polyethylene.  NECAL 8799-45 adheres to many other substrates.

PHYSICAL PROPERTIES

Composition:						Modified Acrylic (low surface energy)

Release Liner:						Available with P or W liners

Thickness:			 			48 mils + or – 10%

Scrim:							Black polyurethane foam

Adhesion: (1)						120-150 oz. /in. (Aluminum/Polypropylene)

340-360 oz. /in. (Aluminum/Stainless)

Tensile: (2)						95 p.s.i., foam failure

Shear Adhesion: (3)					24 hours +

Temperature Range:					Application:  50°F. Minimum

Service:         -20°F to 270°F

(1)  PSTC-1

(2)  Polyester to SS (1 sq.in.)

(3)  1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply to a clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with a dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is at least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

March-13