Technical Data Sheet

NECAL 8899-30 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

8899-30 is a foam supported pressure sensitive adhesive that exhibits very high performance..

FEATURES

8899-30 is primarily intended for use where extreme high performance is needed.  8899-30 has superior impact and vibration resistance.

PHYSICAL PROPERTIES

Composition:						Acrylic

Release Liner:						Available with P or W liner

Thickness:			 			38 mils + or – 10%

Scrim:							Black polyurethane foam

Adhesion: 						80-100 oz./in.

Tensile: 						90 p.s.i.

Shear Adhesion:					7 days +

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

225°F. Maximum

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-09