Technical Data Sheet

NECAL 9180 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

NECAL 9180 is a supported film of pressure sensitive adhesive displaying high performance bond characteristics as well as outstanding initial tack.

FEATURES

NECAL 9180 will adhere to many substrates.

PHYSICAL PROPERTIES

Composition:						Acrylic

Release Liner:						Available with P or W liners

Thickness:			 			3.0 mils (total)

Scrim:							.00048 mil polyester

Adhesion: (1)						220 - 240 oz. /in.

Tensile: (2)						133 p.s.i.

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:  50°F. Minimum

Service:         -40°F. Minimum

195°F. Maximum

(1)  PSTC-1

(2)  Polyester to SS (1 sq.in.)

(3)  1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply to a clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with a dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is at least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

Standard UL 969

This material complies with

Component-Marking and Labeling

System Materials (PGGU2).

March-13