Technical Data Sheet

NECAL 9200 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

NECAL 9200 is an unsupported film of pressure sensitive adhesive that displays high initial tack and peel.

FEATURES

NECAL 9200 will adhere to many substrates including polyethylene and polypropylene.

PHYSICAL PROPERTIES

Composition:						Rubber based

Release Liner:						Available with P or W liners

Thickness:			 			2.0 mils (total)

Adhesion: 						150 - 180 oz. /in.

Tensile: 						100 p.s.i.

Shear Adhesion: 					7 days +

Temperature Range:					Application:  50°F. Minimum

Service:         -40°F. Minimum

170°F. Maximum

BONDING INSTRUCTIONS

Remove the release liner and apply to a clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with a dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is at least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

Standard UL 969

This material complies with

Component-Marking and Labeling

System Materials (PGGU2).

March-13