Technical Data Sheet

NECAL 9375 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

9375 is a supported film of pressure sensitive adhesive displaying excellent bond and initial tack.

FEATURES

9375 will adhere to many substrates including aluminum, brass, steel, glass, enamels and plastics such as polystyrene, ABS, and acrylic.  Because of its thickness 9375 is recommended for use on rough surfaces.

PHYSICAL PROPERTIES

Composition:						Acrylic based adhesive

Release Liner:						Available with P or W liner

Thickness:			 			4.0 mils (total)

Scrim: 							1.0 mil polyester

Adhesion: (1)						325 - 350 oz./in.

Tensile: (2)						180 p.s.i.

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:	60°F. Minimum

Service:	0°F. Minimum

225°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is al least two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values, which will vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION ADHESIVES DIVISION

FOR SAMPLES OR ADDITIONAL INFORMATION

AUGUST-09