Technical Data Sheet

NECAL 9876 PRESSURE SENSITIVE ADHESIVE

DESCRIPTION

9876 is an unsupported film of pressure sensitive adhesive displaying excellent bond characteristics and initial tack.

FEATURES

9876 will adhere to most substrates, including aluminum, brass, steel, glass, enamels and plastics such as polystyrene, ABS and acrylic.  Because of its thickness 9876 is recommended for use on rough surfaces.

PHYSICAL PROPERTIES

Composition:						Acrylic

Release Liner:						Available with P, W, H, HD, or VF liner

Thickness:			 			6.0 mils (total)

Adhesion: (1)						350 - 375 oz./in.

Tensile: (2)						180 p.s.i.

Shear Adhesion: (3)					7 days +

Temperature Range:					Application:	50°F. Minimum

Service:	-40°F. Minimum

225°F. Maximum

(1)	PSTC-1

(2)	Polyester to SS (1 sq.in.)

(3)	1000 grams/sq.in. (polyester to SS)

BONDING INSTRUCTIONS

Remove the release liner and apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is two years when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

AUGUST-10