Technical Data Sheet

NECAL B340-3220 REMOVABLE PRESSURE SENSITIVE ADHESIVE PROTECTIVE FACE MASK

DESCRIPTION

B340-3220 is an unsupported film of removable pressure sensitive adhesive that displays good tack and adhesion but is easily removed with no residue from any surface.

PHYSICAL PROPERTIES

Adhesive:						Acrylic

Carrier:						1.0 mil polyester

Adhesive Thickness:					1.0 mil (Total)

Adhesion:						5-10 oz./in.

Temperature Range:					Application:	50°F. Minimum

Service:	0°F. Minimum

120°F. Maximum

BONDING INSTRUCTIONS

Apply mask to clean, dry substrate.  Use firm pressure to obtain maximum contact.  Use of air, hydraulic or mechanical bonding press is recommended with pressure of 40-60 p.s.i. with dwell time of 2-5 seconds.

STORAGE DATA

The shelf life of this material is one year when stored in a cool, dry place.

NOTICE

The information shown here represents typical values that may vary with each application.  The values are not intended to be a performance guarantee.  Users should determine, prior to use, the suitability of this material for their application.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-10