Technical Data Sheet

NECAL LABEL STOCK

DESCRIPTION

Label Stock is made up of various combinations of face stocks, adhesives and 90 lb. layflat release liner which are manufactured to meet customer requirements.

FEATURES

Label Stock can be manufactured using a variety of Pressure Sensitive Adhesives, which include high temperature acrylic, low surface tension acrylic, a rubber base, general purpose acrylic and others.  It can be supplied with a variety of face stocks, which can include: .001 Brite Chrome PET, .0055 Brite or Brushed Chrome PET, .002 Brite or Brushed Chrome PET, .008 Brite or Brushed Chrome PET.  Other face stocks that those listed above may also be available.

PHYSICAL PROPERTIES

Adhesive:	Acrylic or rubber base

Release Liner:	90 lb. polycoated release liner

AdhesiveThickness:	Can range from ½ mil to 4 mils thick dependent upon

the application.

Adhesion:	Dependent upon adhesive utilized

Tensile:	Dependent upon adhesive utilized

Shear Adhesion:	Dependent upon adhesive utilized

Temperature Range:	Application		50°F. Minimum

Service			-40°F.

Maximum temperature is dependent upon

Adhesive utilized

BONDING INSTRUCTIONS

Remove the release liner and apply to clean, dry substrate.  Use of air, hydraulic or mechanical bonding press is recommended with a pressure of 40-60 P.S.I. with a dwell time of 2 – 5 seconds to insure intimate contact is achieved between nameplate and substrate.

STORAGE DATA

The shelf life of this material is two years when stored in a cool, dry place.

YOU MAY CONTACT NECAL CORPORATION

FOR SAMPLES OR ADDITIONAL INFORMATION

JUNE-10